SUPPLEMENTARY MATERIAL

Diarsine- vs Diphosphine-Protected Au13 Clusters: Effect of Subtle              Geometric Differences on Optical Property and Electronic Structure

Yukatsu Shichibu,1,2,a) Fan Zhang,1 Yuxiang Chen,1 Masafumi Konishi,3 Susumu Tanaka,3 Hiroaki Imoto,3

Kensuke Naka,3 and Katsuaki Konishi1,2,a)

1Graduate School of Environmental Science and 2Faculty of Environmental Earth Science,

Hokkaido University, North 10 West 5, Sapporo 060-0810, Japan.

3Faculty of Molecular Chemistry and Engineering, Graduate School of Science and Technology,

Kyoto Institute of Technology, Goshokaido-cho, Matsugasaki, Sakyo-ku, Kyoto 606-8585, Japan.

I.  Experimental Results

A.  ORTEP Drawing

Figure S1. ORTEP drawing for 3·(SbF6)3. Thermal ellipsoids are drawn at the 50% probability level. For clarity, hydrogen atoms are omitted.

B.  Crystal Data

Table S1. Crystal data for 3·(SbF6)3·5(C7H8)·CH2Cl2.

Empirical formula	C171H172As10Au13Cl4F18Sb3

Formula weight	6385.89 g/mol

Temperature	98 K

Wavelength	1.54184 Å

Crystal size	0.082 × 0.053 × 0.019 mm3

Crystal system	Monoclinic

Space group	C2/c

Unit cell dimensions	a = 31.5214(3) Å	 = 90°

b = 22.12251(16) Å	 = 90.0397(10)°

c = 51.6225(5) Å	 = 90°

Volume	35998.0(5) Å3

Z	8

Density (calculated)	2.357 Mg/m3

Absorption coefficient	25.991 mm-1

F(000)	23504

Theta range for data collection	2.440 to 51.645°

Index ranges	−18 ≤ h ≤ 32, −22 ≤ k ≤ 20, −52 ≤ l ≤ 45

Reflections collected	36069

Independent reflections	16676 [R(int) = 0.0271]

Completeness to theta = 50.38°	85.34 %

Absorption correction	Multi-scan

Max. and min. transmission	1.00000 and 0.27419

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	16676 / 408 / 1826

Goodness-of-fit on F2   	1.085

Reflections with I > 2(I)	14017

Final R indices [I > 2(I)]	R1 = 0.0457, wR2 = 0.1236

R indices (all data)	R1 = 0.0556, wR2 = 0.1291

Largest diff. peak and hole	+2.868 and −1.472 eÅ-3

C.  Angles and Distances of the Pentagonal Antiprismatic Unit

Figure S2. Angles (θ1 and θ2) and distances (d1 and d2) of the pentagonal antiprismatic unit of 3. Areas relating to cross-linked diarsines are shaded in aqua.

D.  Absorption and photoluminescence spectra

Figure S3. Absorption (blue line) and photoluminescence (red line; λex = 450 nm) spectra of 2·Cl3 in MeCN.

II.  Computational Results

A.  Geometry Optimization

Table S2. Average distances (d1, d2, d3, z1 and r1) and angles (θ1 − 36 and θ2 − 36) of the geometry-optimized Au13 clusters (with standard deviations) a

|  |  | d1 (Å) | d2 (Å) | d3 (Å) | z1 (Å) | r1 (Å) | θ1 – 36 (º) | θ2 – 36 (º) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1 | 2.962 ± 0.001 | 3.046 ± 0.002 | 3.046 ± 0.002 | 5.559 | 2.885 ± 0.000 | −1.66 ± 0.07 | +1.66 ± 0.06 |
|  |  | [2.961, 2.963] | [3.043, 3.048] | [3.043, 3.048] |  | [2.884, 2.885] | [−1.79, −1.62] | [+1.55, +1.72] |
|  | 3 | 3.042 ± 0.007 | 3.039 ± 0.033 | 3.039 ± 0.033 | 5.591 | 2.889 ± 0.016 | +0.25 ± 0.45 | −0.25 ± 0.98 |
|  |  | [3.036, 3.054] | [2.985, 3.089] | [2.985, 3.089] |  | [2.863, 2.915] | [−0.41, +0.93] | [−1.57, +1.27] |

a The minimum and maximum values are given in square brackets.

B.  Molecular Orbitals

Figure S4. Selected molecular orbitals of 1. Their assignments as the superatomic P and D orbitals are indicated on the right.

Figure S5. Selected molecular orbitals of 3. Their assignments as the superatomic P and D orbitals are indicated on the right.

C.  Molecular-Orbital and Electron-Transition Data

Table S3. Kohn-Sham orbitals, energies, and atomic orbital contributions of 1.

|  | MO | Orbital index | Orbital energy (eV) / Relative energy (eV) | % Au (sp) | % Au (d) | % P (p) | % Cl (p) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | LUMO+4 | 669a | -7.00 / 3.11 | 61 | 19 | 6 | 12 |
|  | LUMO+3 | 668a | -7.16 / 2.95 | 70 | 3 | 13 | 0 |
|  | LUMO+2 | 667a | -7.16 / 2.95 | 70 | 3 | 13 | 0 |
|  | LUMO+1 | 666a | -7.29 / 2.82 | 70 | 0 | 13 | 1 |
|  | LUMO | 665a | -7.29 / 2.82 | 70 | 0 | 13 | 1 |
|  | HOMO | 664a | -10.11 / 0.00 | 46 | 14 | 19 | 4 |
|  | HOMO-1 | 663a | -10.11 / 0.00 | 45 | 14 | 19 | 4 |
|  | HOMO-2 | 662a | -10.77 / -0.67 | 42 | 16 | 8 | 22 |

Table S4. Kohn-Sham orbitals, energies, and atomic orbital contributions of 3.

|  | MO | Orbital index | Orbital energy (eV) / Relative energy (eV) | % Au (sp) | % Au (d) | % As (p) | % Cl (p) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | LUMO+4 | 779a | -7.19 / 3.10 | 66 | 9 | 9 | 5 |
|  | LUMO+3 | 778a | -7.23 / 3.07 | 69 | 3 | 11 | 1 |
|  | LUMO+2 | 777a | -7.25 / 3.04 | 65 | 11 | 8 | 7 |
|  | LUMO+1 | 776a | -7.36 / 2.94 | 66 | 5 | 12 | 0 |
|  | LUMO | 775a | -7.40 / 2.89 | 66 | 5 | 11 | 0 |
|  | HOMO | 774a | -10.29 / 0.00 | 43 | 13 | 18 | 4 |
|  | HOMO-1 | 773a | -10.30 / -0.01 | 42 | 14 | 18 | 4 |
|  | HOMO-2 | 772a | -10.63 / -0.33 | 41 | 16 | 13 | 13 |

Table S5. Excited states, energies, oscillator strengths and primary orbital-orbital transitions of 1. H-X and L+Y in the nature of transition represent HOMO-X and LUMO+Y, respectively.

|  | Excitation index | Energy (eV) / Wavelength (nm) | Oscillator strength | Dominant transition | Nature of transition |
| --- | --- | --- | --- | --- | --- |
|  | 1 | 2.15 / 577 | 5.24 × 10-8 | 664a→665a, 663a→666a | H→L, H-1→L+1 |
|  | 2 | 2.17 / 571 | 1.45 × 10-6 | 663a→666a, 664a→665a, 663a→665a, 664a→666a | H-1→L+1, H→L, H-1→L, H→L+1 |
|  | 3 | 2.17 / 571 | 3.38 × 10-7 | 664a→666a, 663a→665a, 663a→666a, 664a→665a | H→L+1, H-1→L, H-1→L+1, H→L |
|  | 4 | 2.31 / 536 | 5.55 × 10-5 | 664a→667a, 663a→668a, 663a→667a, 664a→668a | H→L+2, H-1→L+3, H-1→L+2, H→L+3 |
|  | 5 | 2.31 / 536 | 2.36 × 10-5 | 663a→667a, 664a→668a, 664a→667a, 663a→668a | H-1→L+2, H→L+3, H→L+2, H-1→L+3 |
|  | 6 | 2.34 / 529 | 1.01 × 10-1 | 663a→665a, 664a→666a, 663a→666a, 664a→665a | H-1→L, H→L+1, H-1→L+1, H→L |
|  | 7 | 2.36 / 525 | 2.53 × 10-2 | 663a→669a, 664a→668a, 663a→667a | H-1→L+4, H→L+3, H-1→L+2 |
|  | 8 | 2.36 / 525 | 2.52 × 10-2 | 664a→669a, 663a→668a, 664a→667a | H→L+4, H-1→L+3, H→L+2 |
|  | 9 | 2.48 / 501 | 8.38 × 10-2 | 664a→669a, 663a→668a, 664a→667a | H→L+4, H-1→L+3, H→L+2 |
|  | 10 | 2.48 / 501 | 8.33 × 10-2 | 663a→669a, 664a→668a, 663a→667a | H-1→L+4, H→L+3, H-1→L+2 |
|  | 11 | 2.88 / 431 | 8.13 × 10-2 | 662a→665a | H-2→L |
|  | 12 | 2.88 / 431 | 8.09 × 10-2 | 662a→666a | H-2→L+1 |
|  | 13 | 2.96 / 419 | 5.35 × 10-6 | 662a→667a | H-2→L+2 |
|  | 14 | 2.96 / 419 | 5.72 × 10-7 | 662a→668a | H-2→L+3 |

Table S6. Excited states, energies, oscillator strengths and primary orbital-orbital transitions of 3. H-X and L+Y in the nature of transition represent HOMO-X and LUMO+Y, respectively.

|  | Excitation index | Energy (eV) / Wavelength (nm) | Oscillator strength | Dominant transition | Nature of transition |
| --- | --- | --- | --- | --- | --- |
|  | 1 | 2.28 / 544 | 5.28 × 10-3 | 773a→775a, 774a→775a | H-1→L, H→L |
|  | 2 | 2.28 / 543 | 3.13 × 10-3 | 774a→775a, 773a→776a, 773a→775a | H→L, H-1→L+1, H-1→L |
|  | 3 | 2.33 / 532 | 1.66 × 10-2 | 774a→776a, 773a→777a, 774a→777a | H→L+1, H-1→L+2, H→L+2 |
|  | 4 | 2.36 / 526 | 1.04 × 10-2 | 774a→777a, 773a→777a, 773a→776a | H→L+2, H-1→L+2, H-1→L+1 |
|  | 5 | 2.41 / 515 | 2.46 × 10-2 | 774a→778a, 773a→777a | H→L+3, H-1→L+2 |
|  | 6 | 2.43 / 510 | 2.48 × 10-2 | 774a→778a, 773a→777a | H→L+3, H-1→L+2 |
|  | 7 | 2.45 / 506 | 4.57 × 10-3 | 774a→779a, 773a→778a | H→L+4, H-1→L+3 |
|  | 8 | 2.46 / 503 | 7.32 × 10-2 | 774a→777a, 773a→776a | H→L+2, H-1→L+1 |
|  | 9 | 2.49 / 498 | 5.93 × 10-2 | 773a→779a | H-1→L+4 |
|  | 10 | 2.57 / 482 | 8.38 × 10-2 | 774a→779a, 773a→778a, 772a→775a | H→L+4, H-1→L+3, H-2→L |
|  | 11 | 2.59 / 479 | 1.98 × 10-2 | 772a→775a | H-2→L |
|  | 12 | 2.63 / 471 | 5.45 × 10-3 | 772a→776a | H-2→L+1 |
|  | 13 | 2.84 / 437 | 1.32 × 10-1 | 772a→777a | H-2→L+2 |
|  | 14 | 2.85 / 435 | 1.65 × 10-1 | 772a→778a | H-2→L+3 |
|  | 15 | 2.89 / 430 | 7.10 × 10-2 | 772a→779a | H-2→L+4 |