Supplementary Information for:

Factors determining surface oxygen vacancy formation energy in ternary spinel structure oxides with zinc

Yoyo Hinuma1,2*, Shinya Mine 3, Takashi Toyao3,4, Takashi Kamachi4,5, and Ken-ichi Shimizu3,4

1 Department of Energy and Environment, National Institute of Advanced Industrial Science and Technology (AIST), 1-8-31, Midorigaoka, Ikeda 563-8577, Japan

2 Center for Frontier Science, Chiba University, 1-33 Yayoicho, Inage, Chiba 263-8522, Japan

3 Institute for Catalysis, Hokkaido University, N-21, W-10, Kita, Sapporo, Hokkaido 001-0021, Japan

4 Elements Strategy Initiative for Catalysts and Batteries, Kyoto University, Katsura, Nishigyo, Kyoto 615-8520, Japan

5 Department of Life, Environment and Materials Science, Fukuoka Institute of Technology, 3-30-1Wajiro-Higashi, Higashi-ku, Fukuoka 811-0295, Japan

* y.hinuma@aist.go.jp

Table SI-1. Geometry information on slab-and-vacuum models used in this paper.

| Surface (cubic) | Compound | (Å2) | (Å) |  | (Å) |  | Atom count |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Thin | Thick | Thin | Thick | Thin | Thick |
| (100) | ZnAl2O4 | 64.8 | 28.2 | 28.2 | 14.1 | 16.1 | 98 | 112 |
|  | ZnGa2O4 | 69.4 | 29.2 | 29.2 | 14.6 | 16.7 | 98 | 112 |
|  | ZnIn2O4 | 79.9 | 31.3 | 31.3 | 15.6 | 17.9 | 98 | 112 |
|  | ZnV2O4 | 70.8 | 29.4 | 29.4 | 14.7 | 16.8 | 98 | 112 |
|  | ZnCr2O4 | 68.7 | 29.1 | 33.3 | 14.6 | 18.7 | 98 | 126 |
|  | ZnMn2O4 | 68.6 | 29.9 | 29.9 | 15.0 | 17.1 | 98 | 112 |
|  | ZnFe2O4 | 69.9 | 29.2 | 29.2 | 14.6 | 16.7 | 98 | 112 |
|  | ZnCo2O4 | 63.8 | 28.0 | 31.9 | 14.0 | 16.0 | 98 | 112 |
| (110) | ZnAl2O4 | 91.6 | 28.5 | 31.3 | 14.2 | 17.1 | 140 | 168 |
|  | ZnGa2O4 | 98.1 | 29.4 | 32.4 | 14.7 | 17.7 | 140 | 168 |
|  | ZnIn2O4 | 112.9 | 28.4 | 31.6 | 15.8 | 19.0 | 140 | 168 |
|  | ZnV2O4 | 100.2 | 29.7 | 32.6 | 14.8 | 17.8 | 140 | 168 |
|  | ZnCr2O4 | 97.2 | 29.4 | 32.4 | 14.7 | 17.7 | 140 | 168 |
|  | ZnFe2O4 | 98.9 | 29.5 | 32.4 | 14.7 | 17.7 | 140 | 168 |
|  | ZnCo2O4 | 90.2 | 28.2 | 31.1 | 14.1 | 16.9 | 140 | 168 |
| (111) | ZnAl2O4 | 56.1 | 32.5 | 37.2 | 18.6 | 23.2 | 112 | 140 |
|  | ZnGa2O4 | 60.1 | 33.7 | 38.5 | 19.2 | 24.0 | 112 | 140 |
|  | ZnIn2O4 | 69.2 | 36.1 | 41.3 | 20.6 | 25.8 | 112 | 140 |
|  | ZnV2O4 | 61.2 | 34.0 | 38.8 | 19.4 | 24.3 | 112 | 140 |
|  | ZnCr2O4 | 59.7 | 33.6 | 38.3 | 19.2 | 24.0 | 112 | 140 |
|  | ZnMn2O4 | 60.7 | 33.8 | 38.6 | 19.3 | 24.1 | 112 | 140 |
|  | ZnFe2O4 | 60.5 | 33.8 | 38.6 | 19.3 | 24.1 | 112 | 140 |
|  | ZnCo2O4 | 55.2 | 32.3 | 36.9 | 18.4 | 23.1 | 112 | 140 |

Fig. SI-1. Employed terminations ZnM2O4 surfaces other than those shown in Fig. 1 of the main text. Gray, brown, blue, and red balls indicate Zn, spin-up M, spin-down M, and O.

Fig. SI-2. EOvac in eV/defect for various O positions in ZnAl2O4. Grey, blue, and red balls indicate Zn, Al, and O, respectively.

Fig. SI-3. EOvac in eV/defect for various O positions in ZnGa2O4. Grey, blue, and red balls indicate Zn, Ga, and O, respectively.

Fig. SI-4. EOvac in eV/defect for various O positions in ZnIn2O4. Grey, blue, and red balls indicate Zn, In, and O, respectively.

Fig. SI-5. EOvac in eV/defect for various O positions in ZnV2O4. Grey, brown, blue, and red balls indicate Zn, V (spin-up), V (spin-down), and O, respectively. The spin for V is that when cleaved from bulk.

Fig. SI-6. EOvac in eV/defect for various O positions in ZnCr2O4. Grey, brown, blue, and red balls indicate Zn, Cr (spin-up), Cr (spin-down), and O, respectively. The spin for Cr is that when cleaved from bulk.

Fig. SI-7. EOvac in eV/defect for various O positions in ZnMn2O4. Grey, brown, blue, and red balls indicate Zn, Mn (spin-up), Mn (spin-down), and O, respectively. The spin for Mn is that when cleaved from bulk.

Fig. SI-8. EOvac in eV/defect for various O positions in ZnFe2O4. Grey, brown, blue, and red balls indicate Zn, Fe (spin-up), Fe (spin-down), and O, respectively. The spin for Fe is that when cleaved from bulk.

Fig. SI-9. EOvac in eV/defect for various O positions in ZnCo2O4. Grey, blue, and red balls indicate Zn, Co, and O, respectively.

Fig. SI-10. Site-projected DOS of ZnM2O4. The sums of projected DOSs by species and by orbital character are shown. The primitive cell contains two Zn, four M, and eight O atoms. For spin polarized systems (M=V, Cr, Mn, and Fe), only the spin up DOS is shown and the spin up DOS are drawn separately as M(Maj) and M(Min) for the two pairs of M atoms where spin up is the majority and minority spin, respectively. The arrow in ZnV2O4 indicates the bottom of the V minority 3d (t2g) band.

Fig. SI-11. Plots of EOvac versus the absolute value of the Bader charge at the desorbing O site for each ZnM2O4. Points are labelled by orientation, and the least-squares fit line is over all points.

Fig. SI-12. Plots of EOvac versus average O-cation bond length at the desorbing O site for each ZnM2O4. Points are labelled by orientation, and the least-squares fit line is over all points.

Fig. SI-13. Plots of EOvac versus coordination number at the desorbing O site for each ZnM2O4. Points are labelled by orientation, and the least-squares fit line is over all points.