Supporting Information

Molecular motion of halogenated ethylammonium / [18]crown-6 supramolecular ions in nickel dithiolate magnetic crystals

Naohiro Hasuo, Kiyonori Takahashi, Kenta Kokado, Ichiro Hisaki, and Takayoshi Nakamura

Table of Contents

§1. Crystal data, data collection and reduction parameter.

§2. Crystallographically independent molecules with atom numbering

§3. Packing structures of crystals 2-4.

§4. Detailed analysis of structures of crystals 1-4.

§5. Temperature- and frequency-dependent dielectric constants for crystals 1-4

§6. Transfer integrals between [Ni(dmit)2]– molecules in crystals 1-4.

§1. Crystal data, crystal data, data collection, and reduction parameter.

Table S1.  Crystal data, data collection, and reduction parameter for crystals 1, 2, 3 and 4 at the lowest temperatures.

|  | 1@113K | 2@93K | 3@93K | 4@106K |
| --- | --- | --- | --- | --- |
| Temperature / K | 113 | 93 | 93 | 106 |
| Crystal Dimensions / mm3 | 0.724×0.378×0.207 | 0.507×0.211×0.090 | 0.69×0.60×0.18 | 0.40×0.11×0.07 |
| Chemical formula | C20H32NNiO6S10 | C20H31FNNiO6S10 | C20H31ClNNiO6S10 | C20H31BrNNiO6S10 |
| Formula weight | 761.77 | 779.77 | 796.22 | 840.73 |
| Crystal System | Triclinic | Triclinic | Triclinic | Triclinic |
| Space group | P-1 | P-1 | P-1 | P-1 |
| a / Å | 11.1765(4) | 10.3645(3) | 11.2107(3) | 10.9869(3) |
| b / Å | 12.2812(3) | 12.6254(5) | 12.3150(2) | 12.0485(4) |
| c / Å | 12.6527(4) | 12.9123(4) | 12.7451(3) | 13.7559(5) |
| α / deg | 87.364(2) | 69.835(3) | 92.2792(18) | 115.833(4) |
| β / deg | 68.465(3) | 79.972(3) | 112.126(2) | 91.587(3) |
| γ / deg | 80.094(2) | 79.948(3) | 96.0601(18) | 100.906(3) |
| V / Å3 | 1591.12(9) | 1549.82(10) | 1614.83(7) | 1596.83(10) |
| Z | 2 | 2 | 2 | 2 |
| Dcalc / g∙cm-3 | 1.590 | 1.671 | 1.638 | 1.748 |
| μ(Mo Kα) / cm-1 | 1.302 | 1.343 | 1.366 | 2.549 |
| 2max / deg | 61.784 | 61.986 | 61.838 | 61.140 |
| Reflections measured | 22773 | 18605 | 45358 | 19669 |
| Independent reflections | 7934 | 7679 | 8651 | 7891 |
| Reflections used | 7934 | 7679 | 8651 | 7891 |
| R1 a | 0.0357 | 0.0324 | 0.0495 | 0.0356 |
| Rw (F2) b | 0.0980 | 0.0792 | 0.1395 | 0.0703 |
| GOF | 1.051 | 1.070 | 1.098 | 0.995 |
| CCDC number | 2053279 | 2053282 | 2053390 | 2053298 |

a R1 = ∑||Fo| - |Fc|| / ∑|Fo| and b Rw = (∑ω(|Fo| - |Fc|)2 / ∑ωFo2)1/2.

Table S2.  Crystal data, data collection, and reduction parameter for crystal 1.

| Temperature / K | 293 |
| --- | --- |
| Crystal Dimensions / mm3 | 0.724×0.378×0.207 |
| Chemical formula | C20H32NNiO6S10 |
| Formula weight | 761.77 |
| Crystal System | Triclinic |
| Space group | P-1 |
| a / Å | 11.2486(6) |
| b / Å | 12.3540(8) |
| c / Å | 12.7375(8) |
| α / deg | 87.498(5) |
| β / deg | 69.343(6) |
| γ / deg | 80.758(5) |
| V / Å3 | 1634.62(18) |
| Z | 2 |
| Dcalc / g∙cm-3 | 1.548 |
| μ(Mo Kα) / cm-1 | 1.267 |
| 2max / deg | 62.114 |
| Reflections measured | 20189 |
| Independent reflections | 8034 |
| Reflections used | 8034 |
| R1 a | 0.0365 |
| Rw (F2) b | 0.0945 |
| GOF | 1.051 |
| CCDC number | 2053280 |

a R1 = ∑||Fo| - |Fc|| / ∑|Fo| and b Rw = (∑ω(|Fo| - |Fc|)2 / ∑ωFo2)1/2.

Table S3.  Crystal data, data collection, and reduction parameter for crystal 2 at different temperatures.

|  | 2 |  |  |  |
| --- | --- | --- | --- | --- |
| Temperature / K | 113 | 133 | 153 | 173 |
| Crystal Dimensions / mm3 | 0.507×0.211×0.090 | 0.507×0.211×0.090 | 0.507×0.211×0.090 | 0.507×0.211×0.090 |
| Chemical formula | C20H31FNNiO6S10 | C20H31FNNiO6S10 | C20H31FNNiO6S10 | C20H31FNNiO6S10 |
| Formula weight | 779.77 | 779.77 | 779.77 | 779.77 |
| Crystal System | Triclinic | Triclinic | Triclinic | Triclinic |
| Space group | P-1 | P-1 | P-1 | P-1 |
| a / Å | 10.3864(2) | 10.3884(3) | 10.3994(3) | 10.4067(3) |
| b / Å | 12.6343(5) | 12.6271(4) | 12.6286(5) | 12.6314(5) |
| c / Å | 12.9338(5) | 12.9344(4) | 12.9431(4) | 12.9479(4) |
| α / deg | 69.944(3) | 70.113(3) | 70.317(3) | 70.517(3) |
| β / deg | 79.973(3) | 79.966(2) | 79.956(2) | 79.892(2) |
| γ / deg | 79.970(3) | 80.068(2) | 80.078(3) | 80.138(3) |
| V / Å3 | 1557.90(10) | 1559.30(9) | 1564.10(9) | 1567.96(9) |
| Z | 2 | 2 | 2 | 2 |
| Dcalc / g∙cm-3 | 1.662 | 1.661 | 1.656 | 1.650 |
| μ(Mo Kα) / cm-1 | 1.336 | 1.335 | 1.331 | 1.327 |
| 2max / deg | 62.114 | 61.916 | 61.652 | 61.248 |
| Reflections measured | 19702 | 19502 | 19288 | 19026 |
| Independent reflections | 7645 | 7689 | 7694 | 7718 |
| Reflections used | 7645 | 7689 | 7694 | 7718 |
| R1 a | 0.0329 | 0.0386 | 0.0340 | 0.0366 |
| Rw (F2) b | 0.0806 | 0.0941 | 0.0865 | 0.0925 |
| GOF | 1.054 | 0.990 | 1.075 | 1.075 |
| CCDC number | 2053283 | 2053284 | 2053285 | 2053286 |

a R1 = ∑||Fo| - |Fc|| / ∑|Fo| and b Rw = (∑ω(|Fo| - |Fc|)2 / ∑ωFo2)1/2.

|  | 2 |  |  |  |
| --- | --- | --- | --- | --- |
| Temperature / K | 193 | 213 | 233 | 253 |
| Crystal Dimensions / mm3 | 0.507×0.211×0.090 | 0.507×0.211×0.090 | 0.507×0.211×0.090 | 0.507×0.211×0.090 |
| Chemical formula | C20H31FNNiO6S10 | C20H31FNNiO6S10 | C20H31FNNiO6S10 | C20H31FNNiO6S10 |
| Formula weight | 779.77 | 779.77 | 779.77 | 779.77 |
| Crystal System | Triclinic | Triclinic | Triclinic | Triclinic |
| Space group | P-1 | P-1 | P-1 | P-1 |
| a / Å | 10.4204(3) | 10.4363(3) | 10.4520(3) | 10.4754(3) |
| b / Å | 12.6319(4) | 12.6370(4) | 12.6374(4) | 12.6503(4) |
| c / Å | 12.9511(4) | 12.9511(4) | 12.9527(4) | 12.9637(4) |
| α / deg | 70.735(3) | 70.974(3) | 71.178(3) | 71.385(3) |
| β / deg | 79.898(2) | 79.852(2) | 79.806(2) | 79.802(2) |
| γ / deg | 80.250(2) | 80.316(2) | 80.408(2) | 80.550(2) |
| V / Å3 | 1572.90(9) | 1578.17(8) | 1582.77(9) | 1591.61(9) |
| Z | 2 | 2 | 2 | 2 |
| Dcalc / g∙cm-3 | 1.646 | 1.641 | 1.636 | 1.627 |
| μ(Mo Kα) / cm-1 | 1.323 | 1.319 | 1.315 | 1.308 |
| 2max / deg | 61.70 | 61.50 | 62.07 | 61.34 |
| Reflections measured | 19734 | 19305 | 19876 | 19688 |
| Independent reflections | 7797 | 7814 | 7847 | 7844 |
| Reflections used | 7797 | 7814 | 7847 | 7844 |
| R1 a | 0.0414 | 0.0336 | 0.0335 | 0.0343 |
| Rw (F2) b | 0.1011 | 0.0838 | 0.0864 | 0.0810 |
| GOF | 1.016 | 1.050 | 1.044 | 1.047 |
| CCDC number | 2053287 | 2053288 | 2053289 | 2053290 |

a R1 = ∑||Fo| - |Fc|| / ∑|Fo| and b Rw = (∑ω(|Fo| - |Fc|)2 / ∑ωFo2)1/2.

|  | 2 |  |  |  |
| --- | --- | --- | --- | --- |
| Temperature / K | 273 | 293 | 313 | 333 |
| Crystal Dimensions / mm3 | 0.507×0.211×0.090 | 0.507×0.211×0.090 | 0.507×0.211×0.090 | 0.507×0.211×0.090 |
| Chemical formula | C20H31FNNiO6S10 | C20H31FNNiO6S10 | C20H31FNNiO6S10 | C20H31FNNiO6S10 |
| Formula weight | 779.77 | 779.77 | 779.77 | 779.77 |
| Crystal System | Triclinic | Triclinic | Triclinic | Triclinic |
| Space group | P-1 | P-1 | P-1 | P-1 |
| a / Å | 10.4883(2) | 10.5115(3) | 10.5377(3) | 10.5475(3) |
| b / Å | 12.6467(3) | 12.6531(4) | 12.6697(3) | 12.6632(3) |
| c / Å | 12.9675(3) | 12.9821(3) | 13.0079(4) | 13.0124(4) |
| α / deg | 71.543(2) | 71.701(2) | 71.903(2) | 72.091(3) |
| β / deg | 79.792(2) | 79.787(2) | 79.822(2) | 79.842(3) |
| γ / deg | 80.656(2) | 80.782(2) | 80.956(2) | 81.154(2) |
| V / Å3 | 1595.30(6) | 1603.24(8) | 1615.05(8) | 1618.65(8) |
| Z | 2 | 2 | 2 | 2 |
| Dcalc / g∙cm-3 | 1.623 | 1.615 | 1.603 | 1.600 |
| μ(Mo Kα) / cm-1 | 1.305 | 1.298 | 1.289 | 1.286 |
| 2max / deg | 61.89 | 61.438 | 58.006 | 57.812 |
| Reflections measured | 39570 | 20112 | 17913 | 19117 |
| Independent reflections | 8451 | 7909 | 7336 | 7320 |
| Reflections used | 8451 | 7909 | 7336 | 7320 |
| R1 a | 0.0357 | 0.0336 | 0.0354 | 0.0383 |
| Rw (F2) b | 0.1327 | 0.0801 | 0.0855 | 0.0986 |
| GOF | 0.870 | 1.055 | 1.042 | 1.077 |
| CCDC number | 2053291 | 2053292 | 2053293 | 2053294 |

a R1 = ∑||Fo| - |Fc|| / ∑|Fo| and b Rw = (∑ω(|Fo| - |Fc|)2 / ∑ωFo2)1/2.

|  | 2 |  |
| --- | --- | --- |
| Temperature / K | 353 | 373 |
| Crystal Dimensions / mm3 | 0.507×0.211×0.090 | 0.507×0.211×0.090 |
| Chemical formula | C20H31FNNiO6S10 | C20H31FNNiO6S10 |
| Formula weight | 779.77 | 779.77 |
| Crystal System | Triclinic | Triclinic |
| Space group | P-1 | P-1 |
| a / Å | 10.5673(4) | 10.5742(7) |
| b / Å | 12.6724(4) | 12.6426(7) |
| c / Å | 13.0358(6) | 13.0305(11) |
| α / deg | 72.219(4) | 72.446(6) |
| β / deg | 79.801(4) | 79.808(6) |
| γ / deg | 81.293(3) | 81.420(5) |
| V / Å3 | 1627.17(12) | 1626.1(2) |
| Z | 2 | 2 |
| Dcalc / g∙cm-3 | 1.592 | 1.593 |
| μ(Mo Kα) / cm-1 | 1.279 | 1.280 |
| 2max / deg | 58.162 | 58.054 |
| Reflections measured | 18534 | 18911 |
| Independent reflections | 7331 | 7413 |
| Reflections used | 7331 | 7413 |
| R1 a | 0.0459 | 0.0514 |
| Rw (F2) b | 0.1373 | 0.1505 |
| GOF | 0.911 | 0.911 |
| CCDC number | 2053295 | 2053296 |

a R1 = ∑||Fo| - |Fc|| / ∑|Fo| and b Rw = (∑ω(|Fo| - |Fc|)2 / ∑ωFo2)1/2.

Table S4.  Crystal data, data collection, and reduction parameter for crystal 3 at different temperatures.

|  | 3 |  |  |  |
| --- | --- | --- | --- | --- |
| Temperature / K | 113 | 133 | 153 | 173 |
| Crystal Dimensions / mm3 | 0.69×0.60×0.18 | 0.69×0.60×0.18 | 0.69×0.60×0.18 | 0.290×0.249×0.157 |
| Chemical formula | C20H31ClNNiO6S10 | C20H31ClNNiO6S10 | C20H31ClNNiO6S10 | C20H31ClNNiO6S10 |
| Formula weight | 796.22 | 796.22 | 796.22 | 796.22 |
| Crystal System | Triclinic | Triclinic | Triclinic | Triclinic |
| Space group | P-1 | P-1 | P-1 | P-1 |
| a / Å | 11.2193(3) | 11.2216(3) | 11.2185(3) | 11.2452(2) |
| b / Å | 12.3191(2) | 12.3162(3) | 12.3084(3) | 12.3442(2) |
| c / Å | 12.7473(3) | 12.7541(3) | 12.7536(3) | 12.8113(2) |
| α / deg | 92.239(2) | 92.155(2) | 92.083(2) | 91.8320(10) |
| β / deg | 111.956(2) | 111.864(2) | 111.733(2) | 111.4310(10) |
| γ / deg | 96.066(2) | 96.100(2) | 96.128(2) | 96.2430(10) |
| V / Å3 | 1618.98(7) | 1620.96(7) | 1621.02(7) | 1640.65(5) |
| Z | 2 | 2 | 2 | 2 |
| Dcalc / g∙cm-3 | 1.633 | 1.631 | 1.631 | 1.612 |
| μ(Mo Kα) / cm-1 | 1.363 | 1.361 | 1.361 | 7.865 |
| 2max / deg | 52.742 | 52.744 | 61.84 | 144.97 |
| Reflections measured | 37298 | 35045 | 41879 | 39675 |
| Independent reflections | 6613 | 6623 | 8598 | 6266 |
| Reflections used | 6613 | 6623 | 8598 | 6266 |
| R1 a | 0.0446 | 0.0419 | 0.0438 | 0.0385 |
| Rw (F2) b | 0.1268 | 0.1168 | 0.1217 | 0.1156 |
| GOF | 1.077 | 1.056 | 1.068 | 1.020 |
| CCDC number | 2053392 | 2053393 | 2053394 | 2053395 |

a R1 = ∑||Fo| - |Fc|| / ∑|Fo| and b Rw = (∑ω(|Fo| - |Fc|)2 / ∑ωFo2)1/2.

|  | 3 |  |  |  |
| --- | --- | --- | --- | --- |
| Temperature / K | 193 | 213 | 233 | 253 |
| Crystal Dimensions / mm3 | 0.371×0.624×0.961 | 0.290×0.249×0.157 | 0.290×0.249×0.157 | 0.290×0.249×0.157 |
| Chemical formula | C20H31ClNNiO6S10 | C20H31ClNNiO6S10 | C20H31ClNNiO6S10 | C20H31ClNNiO6S10 |
| Formula weight | 796.22 | 796.22 | 796.22 | 796.22 |
| Crystal System | Triclinic | Triclinic | Triclinic | Triclinic |
| Space group | P-1 | P-1 | P-1 | P-1 |
| a / Å | 11.25474(18) | 11.2637(2) | 11.27140(10) | 11.27840(10) |
| b / Å | 12.34881(18) | 12.34200(10) | 12.34060(10) | 12.34600(10) |
| c / Å | 12.82304(17) | 12.8337(2) | 12.84520(10) | 12.86190(10) |
| α / deg | 91.7415(11) | 91.3720(10) | 91.2410(10) | 91.1450(10) |
| β / deg | 111.2915(14) | 110.9960(10) | 110.8230(10) | 110.6780(10) |
| γ / deg | 96.3016(12) | 96.4500(10) | 96.4520(10) | 96.4220(10) |
| V / Å3 | 1645.75(4) | 1651.13(4) | 1655.78(3) | 1661.63(3) |
| Z | 2 | 2 | 2 | 2 |
| Dcalc / g∙cm-3 | 1.607 | 1.602 | 1.597 | 1.591 |
| μ(Mo Kα) / cm-1 | 1.341 | 7.815 | 7.793 | 7.765 |
| 2max / deg | 58.252 | 145.476 | 146.17 | 144.498 |
| Reflections measured | 33190 | 42270 | 41408 | 41385 |
| Independent reflections | 7803 | 6349 | 6351 | 6340 |
| Reflections used | 7803 | 6349 | 6351 | 6340 |
| R1 a | 0.0347 | 0.0310 | 0.0321 | 0.0271 |
| Rw (F2) b | 0.0910 | 0.0815 | 0.0845 | 0.0763 |
| GOF | 1.084 | 1.034 | 1.052 | 1.053 |
| CCDC number | 2053396 | 2053397 | 2053398 | 2053399 |

a R1 = ∑||Fo| - |Fc|| / ∑|Fo| and b Rw = (∑ω(|Fo| - |Fc|)2 / ∑ωFo2)1/2.

|  | 3 |  |  |  |
| --- | --- | --- | --- | --- |
| Temperature / K | 273 | 293 | 313 | 333 |
| Crystal Dimensions / mm3 | 0.69×0.60×0.18 | 0.371×0.624×0.961 | 0.371×0.624×0.961 | 0.69×0.60×0.18 |
| Chemical formula | C20H31ClNNiO6S10 | C20H31ClNNiO6S10 | C20H31ClNNiO6S10 | C20H31ClNNiO6S10 |
| Formula weight | 796.22 | 796.22 | 796.22 | 796.22 |
| Crystal System | Triclinic | Triclinic | Triclinic | Triclinic |
| Space group | P-1 | P-1 | P-1 | P-1 |
| a / Å | 11.2803(3) | 11.2892(3) | 11.3149(3) | 11.3046(5) |
| b / Å | 12.3375(2) | 12.3438(3) | 12.3589(3) | 12.3319(4) |
| c / Å | 12.8611(3) | 12.8805(3) | 12.9090(3) | 12.9008(6) |
| α / deg | 91.103(2) | 91.047(2) | 90.9686(19) | 90.991(3) |
| β / deg | 110.634(2) | 110.467(2) | 110.340(2) | 110.208(4) |
| γ / deg | 96.375(2) | 96.326(2) | 96.269(2) | 96.173(3) |
| V / Å3 | 1661.43(7) | 1668.26(7) | 1679.59(8) | 1675.11(13) |
| Z | 2 | 2 | 2 | 2 |
| Dcalc / g∙cm-3 | 1.592 | 1.583 | 1.574 | 1.579 |
| μ(Mo Kα) / cm-1 | 1.328 | 1.322 | 1.314 | 1.317 |
| 2max / deg | 62.142 | 58.016 | 58.032 | 52.744 |
| Reflections measured | 49247 | 32304 | 32926 | 27105 |
| Independent reflections | 8848 | 7906 | 7989 | 6845 |
| Reflections used | 8848 | 7906 | 7989 | 6845 |
| R1 a | 0.0389 | 0.0366 | 0.0389 | 0.0516 |
| Rw (F2) b | 0.1292 | 0.1064 | 0.1150 | 0.1420 |
| GOF | 1.015 | 1.015 | 0.996 | 0.986 |
| CCDC number | 2053391 | 2053400 | 2053401 | 2053402 |

a R1 = ∑||Fo| - |Fc|| / ∑|Fo| and b Rw = (∑ω(|Fo| - |Fc|)2 / ∑ωFo2)1/2.

|  | 3 |  |
| --- | --- | --- |
| Temperature / K | 353 | 373 |
| Crystal Dimensions / mm3 | 0.69×0.60×0.18 | 0.371×0.624×0.961 |
| Chemical formula | C20H31ClNNiO6S10 | C20H31ClNNiO6S10 |
| Formula weight | 796.22 | 796.22 |
| Crystal System | Triclinic | Triclinic |
| Space group | P-1 | P-1 |
| a / Å | 11.3244(5) | 11.3571(2) |
| b / Å | 12.3495(4) | 12.3603(2) |
| c / Å | 12.9385(6) | 12.9511(3) |
| α / deg | 90.918(3) | 90.864(2) |
| β / deg | 110.128(4) | 109.988(2) |
| γ / deg | 96.018(3) | 95.958(2) |
| V / Å3 | 1686.95(13) | 1696.81(6) |
| Z | 2 | 2 |
| Dcalc / g∙cm-3 | 1.568 | 1.558 |
| μ(Mo Kα) / cm-1 | 1.308 | 1.300 |
| 2max / deg | 58.424 | 58.26 |
| Reflections measured | 30129 | 33505 |
| Independent reflections | 8054 | 8059 |
| Reflections used | 8054 | 8059 |
| R1 a | 0.0559 | 0.0396 |
| Rw (F2) b | 0.1553 | 0.1222 |
| GOF | 0.916 | 0.968 |
| CCDC number | 2053403 | 2053404 |

a R1 = ∑||Fo| - |Fc|| / ∑|Fo| and b Rw = (∑ω(|Fo| - |Fc|)2 / ∑ωFo2)1/2.

Table S5.  Crystal data, data collection, and reduction parameter for crystal 4 at different temperatures.

|  | 4 |  |  |  |
| --- | --- | --- | --- | --- |
| Temperature / K | 113 | 133 | 153 | 173 |
| Crystal Dimensions / mm3 | 0.40×0.11×0.07 | 0.40×0.11×0.07 | 0.40×0.11×0.07 | 0.40×0.11×0.07 |
| Chemical formula | C20H31BrNNiO6S10 | C20H31BrNNiO6S10 | C20H31BrNNiO6S10 | C20H31BrNNiO6S10 |
| Formula weight | 840.68 | 840.68 | 840.68 | 840.68 |
| Crystal System | Triclinic | Triclinic | Triclinic | Triclinic |
| Space group | P-1 | P-1 | P-1 | P-1 |
| a / Å | 10.9810(3) | 11.0117(3) | 11.0165(3) | 11.0374(3) |
| b / Å | 12.0448(3) | 12.0652(3) | 12.0569(4) | 12.0627(3) |
| c / Å | 13.7409(4) | 13.7791(4) | 13.7786(4) | 13.7656(4) |
| α / deg | 115.825(3) | 115.895(3) | 64.116(3) | 64.349(3) |
| β / deg | 91.535(2) | 91.351(2) | 79.239(3) | 79.574(2) |
| γ / deg | 100.927(2) | 101.004(2) | 78.965(2) | 78.920(2) |
| V / Å3 | 1593.91(8) | 1604.68(8) | 1605.03(9) | 1611.42(9) |
| Z | 2 | 2 | 2 | 2 |
| Dcalc / g∙cm-3 | 1.747 | 1.740 | 1.739 | 1.733 |
| μ(Mo Kα) / cm-1 | 2.554 | 2.537 | 2.536 | 2.526 |
| 2max / deg | 62.086 | 61.834 | 62.064 | 62.062 |
| Reflections measured | 38281 | 38326 | 39974 | 40700 |
| Independent reflections | 8378 | 8423 | 8484 | 8560 |
| Reflections used | 8378 | 8423 | 8484 | 8560 |
| R1 a | 0.0315 | 0.0325 | 0.0337 | 0.0333 |
| Rw (F2) b | 0.0677 | 0.0677 | 0.0706 | 0.0690 |
| GOF | 1.016 | 1.026 | 1.032 | 1.039 |
| CCDC number | 2053299 | 2053300 | 2053301 | 2053302 |

a R1 = ∑||Fo| - |Fc|| / ∑|Fo| and b Rw = (∑ω(|Fo| - |Fc|)2 / ∑ωFo2)1/2.

|  | 4 |  |  |  |
| --- | --- | --- | --- | --- |
| Temperature / K | 193 | 213 | 233 | 253 |
| Crystal Dimensions / mm3 | 0.40×0.11×0.07 | 0.40×0.11×0.07 | 0.40×0.11×0.07 | 0.40×0.11×0.07 |
| Chemical formula | C20H31BrNNiO6S10 | C20H31BrNNiO6S10 | C20H31BrNNiO6S10 | C20H31BrNNiO6S10 |
| Formula weight | 840.68 | 840.68 | 840.68 | 840.68 |
| Crystal System | Triclinic | Triclinic | Triclinic | Triclinic |
| Space group | P-1 | P-1 | P-1 | P-1 |
| a / Å | 11.0467(3) | 11.0537(3) | 11.0760(3) | 11.0864(3) |
| b / Å | 12.0603(3) | 12.0557(3) | 12.0662(3) | 12.0734(3) |
| c / Å | 13.7505(4) | 13.7262(4) | 13.7164(5) | 13.7103(4) |
| α / deg | 64.635(3) | 64.890(3) | 65.106(3) | 65.253(3) |
| β / deg | 79.967(2) | 80.331(2) | 80.573(3) | 80.773(3) |
| γ / deg | 78.865(2) | 78.815(2) | 78.719(2) | 78.660(2) |
| V / Å3 | 1615.49(8) | 1617.26(9) | 1623.84(9) | 1627.77(9) |
| Z | 2 | 2 | 2 | 2 |
| Dcalc / g∙cm-3 | 1.728 | 1.726 | 1.719 | 1.715 |
| μ(Mo Kα) / cm-1 | 2.520 | 2.517 | 2.507 | 2.501 |
| 2max / deg | 62.048 | 62.122 | 62.116 | 62.16 |
| Reflections measured | 40000 | 40716 | 40270 | 42066 |
| Independent reflections | 8603 | 8593 | 8614 | 8660 |
| Reflections used | 8603 | 8593 | 8614 | 8660 |
| R1 a | 0.0375 | 0.0391 | 0.0405 | 0.0377 |
| Rw (F2) b | 0.0851 | 0.0818 | 0.0923 | 0.0875 |
| GOF | 1.073 | 1.039 | 1.019 | 1.039 |
| CCDC number | 2053303 | 2053304 | 2053305 | 2053306 |

a R1 = ∑||Fo| - |Fc|| / ∑|Fo| and b Rw = (∑ω(|Fo| - |Fc|)2 / ∑ωFo2)1/2.

|  | 4 |  |  |  |
| --- | --- | --- | --- | --- |
| Temperature / K | 273 | 293 | 313 | 333 |
| Crystal Dimensions / mm3 | 0.40×0.11×0.07 | 0.40×0.11×0.07 | 0.40×0.11×0.07 | 0.40×0.11×0.07 |
| Chemical formula | C20H31BrNNiO6S10 | C20H31BrNNiO6S10 | C20H31BrNNiO6S10 | C20H31BrNNiO6S10 |
| Formula weight | 840.68 | 840.68 | 840.68 | 840.68 |
| Crystal System | Triclinic | Triclinic | Triclinic | Triclinic |
| Space group | P-1 | P-1 | P-1 | P-1 |
| a / Å | 11.1022(4) | 11.1201(5) | 11.1694(4) | 11.1865(5) |
| b / Å | 12.0838(4) | 12.1021(5) | 12.1413(4) | 12.1459(5) |
| c / Å | 13.7055(5) | 13.7058(7) | 13.7408(6) | 13.7395(6) |
| α / deg | 65.348(3) | 65.393(5) | 65.543(4) | 65.630(4) |
| β / deg | 80.897(3) | 80.958(4) | 81.123(3) | 81.204(4) |
| γ / deg | 78.557(3) | 78.454(4) | 78.362(3) | 78.269(4) |
| V / Å3 | 1632.00(11) | 1637.40(15) | 1656.09(12) | 1659.95(14) |
| Z | 2 | 2 | 2 | 2 |
| Dcalc / g∙cm-3 | 1.709 | 1.705 | 1.686 | 1.682 |
| μ(Mo Kα) / cm-1 | 2.494 | 2.486 | 2.458 | 2.452 |
| 2max / deg | 62.156 | 62.106 | 58.064 | 58.072 |
| Reflections measured | 41574 | 42141 | 33146 | 34340 |
| Independent reflections | 8724 | 8744 | 7890 | 7868 |
| Reflections used | 8724 | 8744 | 7890 | 7868 |
| R1 a | 0.0413 | 0.0431 | 0.0416 | 0.0879 |
| Rw (F2) b | 0.0922 | 0.0958 | 0.0958 | 0.1086 |
| GOF | 1.020 | 1.031 | 1.049 | 1.027 |
| CCDC number | 2053307 | 2053308 | 2053309 | 2053310 |

a R1 = ∑||Fo| - |Fc|| / ∑|Fo| and b Rw = (∑ω(|Fo| - |Fc|)2 / ∑ωFo2)1/2.

.

|  | 4 |  |
| --- | --- | --- |
| Temperature / K | 353 | 373 |
| Crystal Dimensions / mm3 | 0.40×0.11×0.07 | 0.40×0.11×0.07 |
| Chemical formula | C20H31BrNNiO6S10 | C20H31BrNNiO6S10 |
| Formula weight | 840.68 | 840.68 |
| Crystal System | Triclinic | Triclinic |
| Space group | P-1 | P-1 |
| a / Å | 11.2110(4) | 11.2167(4) |
| b / Å | 12.1703(4) | 12.1808(4) |
| c / Å | 13.7456(5) | 13.7373(5) |
| α / deg | 65.635(3) | 65.696(3) |
| β / deg | 81.252(3) | 81.308(3) |
| γ / deg | 78.145(3) | 78.012(3) |
| V / Å3 | 1667.21(10) | 1668.72(11) |
| Z | 2 | 2 |
| Dcalc / g∙cm-3 | 1.675 | 1.673 |
| μ(Mo Kα) / cm-1 | 2.442 | 2.439 |
| 2max / deg | 58.086 | 58.11 |
| Reflections measured | 34600 | 35265 |
| Independent reflections | 7944 | 7932 |
| Reflections used | 7944 | 7932 |
| R1 a | 0.0522 | 0.0470 |
| Rw (F2) b | 0.1284 | 0.1118 |
| GOF | 1.016 | 1.008 |
| CCDC number | 2053311 | 2053312 |

a R1 = ∑||Fo| - |Fc|| / ∑|Fo| and b Rw = (∑ω(|Fo| - |Fc|)2 / ∑ωFo2)1/2.

§2. Crystallographically independent molecules with atom numbering

Figure S1. Crystallographically independent molecules in the crystal 1 at 113 K with atomic numbers. Crystallographically independent molecular structure is depicted as ORTEP with 50% thermal ellipsoids probability level. Hydrogen atoms are omitted for clarity.

Figure S2. Crystallographically independent molecules in the crystal 2 at 93 K with atomic numbers. The structure is depicted as ORTEP with 50% probability. Hydrogen atoms are omitted for clarity.

Figure S3. Crystallographically independent molecules in the crystal 3 at 93 K with atomic numbers. The structure is depicted as ORTEP with 50% probability. Hydrogen atoms are omitted for clarity.

Figure S4. Crystallographically independent molecules in the crystal 4 at 293 K with atomic numbers. The structure is depicted as ORTEP with 50% probability. Hydrogen atoms are omitted for clarity.

§3. Packing structures of crystals 2-4.

Figure S5. Packing structures of crystals 2, 3 and 4 viewed along the (a) c, (c) c and (e) b axis, respectively. 2D arrangement of supramolecular cations for crystals 2, 3 and 4 viewed along the (b) b, (d) b and (f) c axis, respectively. Dotted square encircles the 1D arrangement of supramolecular cations. Hydrogen atoms are omitted for clarity except the atoms connected to nitrogen atom. Sulfur, carbon, and nickel atoms in [Ni(dmit)2] colored as yellow, grey, and green, respectively. Yellow X-C2-NH3 and blue [18]crown-6, and red X-C2-NH3 and green [18]crown-6 is supramolecular cation unit and the two unit form supramolecular cation pair.

§4. Detailed analysis of structures of crystal 1-4.

Table S6. Intermolecular interaction between supramolecular cations and density of the crystals at the lowest temperatures.

| Crystals | aInteraction | Å | bdc•••c / Å | Dcalc / g cm3 |
| --- | --- | --- | --- | --- |
| 1 | C-H•••O | 3.595(2) | 3.726 | 1.590 |
| 2 | C-H•••O | 3.633(2) | 3.745 | 1.671 |
| 3 |  |  | 3.782 | 1.638 |
| 4 | C-H•••O | 3.468(3), 3.477(4) | 3.635 | 1.748 |

a Intermolecular interaction between the neighboring supramolecular cations. Instead of H•••O distance, distance of C•••O was used for C-H•••O interaction. Distance of weak hydrogen bonding is in the range of 3.2-4.0 Å between hydrogen-bonded donor•••acceptor atoms.

b Distance between two plane of neighboring [18]crown-6. The plane of [18]crown-6 used by six oxygen atom in [18]crown-6.

§5. Temperature- and frequency-dependent dielectric constants for crystals 1-4

Figure S6. Temperature- and frequency-dependent real part of dielectric constant (ε1) and tangent delta for crystal 1.

Figure S7. Temperature- and frequency-dependent real part of dielectric constant (ε1) and tangent delta for crystal 2.

Figure S8. Temperature- and frequency-dependent real part of dielectric constant (ε1) and tangent delta for crystal 3.

§6. Transfer integrals between [Ni(dmit)2]– molecules in crystals 1-4.

Figure S9. Transfer integral between [Ni(dmit)2]– anions in crystals (a) 1, (b) 2, (c) 3, and (d) 4. t1 corresponds to the transfer integrals between the intradimer [Ni(dmit)2]– anions, whereas t2 and t3 are transfer integrals between interdimer [Ni(dmit)2] anions.