Supplementary material

Extraction of Cs bound with biotite by addition of oxalic acid without heating

Yasuhiro Akemoto1, 2*, Seira Takahashi1, Toko Iwamura1, Masahiko Kan3 and Shunitz Tanaka1, 4, 5*

Table S1 Characteristic of biotite in this study.

| Chemical component | wt% |
| --- | --- |
| SiO2 Al2O3 TiO2 Fe2O3 MgO CaO K2O | 50.3 21.5 2.2 8.9 9.9 1.4 5.8 |

Desorbed elements from biotite

Fig. S1 Desorption rate of elements at each leaching time from biotite by (a) 1.0 mol/L LiNO3 and (b) 0.1 mol/L oxalic acid; Symbols, purple triangle was Fe, blue circle was Mg, red square was Al, and green rhombus was Si, respectively