Supplementary data for the article:

Physicochemical functionality of chimeric isomaltomegalosaccharides with α-(1→4)-glucosidic segments of various lengths

Weeranuch Lang1,*, Yuya Kumagai1, Shinji Habu1, Juri Sadahiro1, Takayoshi Tagami1, Masayuki Okuyama1, Shinichi Kitamura2, Nobuo Sakairi3, Atsuo Kimura1,*

1Research Faculty of Agriculture, Hokkaido University, Sapporo 060-8589, Japan

2Center for Research and Development of Bioresources, Organization for Research Promotion, Osaka Prefecture University, Osaka 599-8531, Japan

3Graduate School of Environmental Science, Hokkaido University, Sapporo 060-0810, Japan

*Corresponding author: tel/fax, +81 11 706 2808; e-mail address, weranuch@abs.agr.hokudai.ac.jp (Weeranuch Lang) and kimura@abs.agr.hokudai.ac.jp (Atsuo Kimura)

Table S1. Moisture content of IMS

| IMS | Moisture content (%)* |
| --- | --- |
| IMS-13/3 | 4.3 |
| IMS-13/6 | 5.4 |
| IMS-15/9 | 4.3 |

* Evaluated from moisture loss at 120 °C by TGA analysis.

Fig. S1. Preparation of G12 from short amylose (DP = 16.5–19.5). A, Preparation procedure of G12. B, Size distribution of maltodextrin fraction in each step analyzed by gel permeation HPLC.

Fig. S2. 1H-NMR spectra of glucosaccharides. A and B, G12 and short amylose (DP = 16.5–19.5); C and D, IMS-13/3, IMS-13/6, IMS-15/9, and IMSs prepared from G4; A and C, spectra covering anomeric proton area. Signal of (2H5)dimethyl sulfoxide was calibrated at δ 4.3706 ppm.

# Fig. S3. Digestion of IMSs by dextran glucosidase. According to our previously reported method (Lang et al., 2022), both enzymatic digestion and separation of products  were conducted. *, internal standard (myo-inositol).

Fig. S4. Benesi-Hildebrand double-reciprocal plots for the determination of Kc values of IMSs. A, IMS-13/3: I value, 39.0–236; I0 value, 14.7. B, IMS-13/6: I value, 72.4–430; I0 value, 14.4. C, IMS-15/9: I value, 97.4–506; I0 value, 14.9. Concentration of IMS used, 1.0–10 mM.