Supporting Information

Uniaxial Negative Thermal Expansion Induced by Molecular Rotation in One-Dimensional Supramolecular Assembly with Associated Peculiar Magnetic Behavior

Kiyonori Takahashi,* Yuki Shirakawa, Hiroki Sakai, Ichiro Hisaki, Shin-ichiro Noro, Tomoyuki Akutagawa, Motohiro Nakano, and Takayoshi Nakamura*

E-mail: ktakahashi@es.hokudai.ac.jp (K. Takahashi), tnaka@es.hokudai.ac.jp (T. Nakamura)

Table of Contents

§1. Crystal data, Crystal Data, Data Collection, and Reduction Parameter.

§2. Crystallographically independent molecules with atom numbering

§3. Input and output file of PASCal Calculation

§4 Differential scanning calorimetry (DSC) for crystal 1

§5 Temperature-dependence of structural change between PD1B•••DB2 and PD1B•••PD2.

§6 Transfer integrals (t) between [Ni(dmit)2]– anions and their temperature dependence.

§7 Expanded χmT versus T plot of Figure 5.

§1. Crystal data, Crystal Data, Data Collection, and Reduction Parameter.

The Flack parameter analyzed for P21 was 0.320(11) at 118 K. Relatively large Flack parameter suggests that the inverted domain, where dipole moment of PD2 are aligned anti-parallel to the first domain, are included in the crystal 1. It is because crystal structure of 1 can be refined by assuming inversion twin and BASF commands in shelx refinement, where volume ratio of twin domains were 0.680(11):0.320(11) at 118 K.

Table S1.  Crystal Data, Data Collection, and Reduction Parameter for crystal 1.

|  | 1 |  |  |  |
| --- | --- | --- | --- | --- |
| Temperature / K | 118 | 135 | 151 | 169 |
| Crystal Dimensions / mm3 | 0.6×0.6×0.6 |  |  |  |
| Chemical formula | C92H106N4Ni2O24S20 |  |  |  |
| Formula weight | 2410.42 |  |  |  |
| Crystal System | Monoclinic |  |  |  |
| Space group | P21 |  |  |  |
| a / Å | 13.0944(2) | 13.1146(2) | 13.1390(2) | 13.1620(3) |
| b / Å | 21.8192(3) | 21.8149(3) | 21.8050(3) | 21.7862(3) |
| c / Å | 18.0486(3) | 18.0621(3) | 18.0856(3) | 18.1119(3) |
| β / deg | 94.6070(15) | 94.502(2) | 94.4155(16) | 94.3187(16) |
| V / Å3 | 5139.99(14) | 5151.51(14) | 5166.08(15) | 5178.82(15) |
| Z | 2 | 2 | 2 | 2 |
| Dcalc / g∙cm-3 | 1.557 | 1.554 | 1.550 | 1.546 |
| μ(Mo Kα) / cm-1 | 0.847 | 0.845 | 0.843 | 0.840 |
| 2max / deg | 62.5200 | 61.8940 | 62.1320 | 61.586 |
| Reflections measured | 77144 | 78128 | 77762 | 80139 |
| Independent reflections | 26132 | 25961 | 25989 | 26243 |
| Reflections used | 26132 | 25961 | 25989 | 26243 |
| R1 a | 0.0350 | 0.0357 | 0.0364 | 0.0374 |
| Rw(F2) a | 0.0803 | 0.0833 | 0.0861 | 0.0888 |
| GOF | 1.026 | 1.034 | 1.041 | 1.039 |
| Flack Parameter | 0.320(11) | 0.334(11) | 0.318(11) | 0.315(11) |
| CCDC No. | 2163119 | 2163120 | 2163121 | 2163122 |

a R1 = ||Fo| - |Fc|| / |Fo| and Rw = (|Fo| - |Fc|)2 / Fo2)1/2.

|  | 1 |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Temperature / K | 177 | 186 | 194 | 202 | 221 |
| Crystal Dimensions / mm3 | 0.6×0.6×0.6 |  |  |  |  |
| Chemical formula | C92H106N4Ni2O24S20 |  |  |  |  |
| Formula weight | 2410.42 |  |  |  |  |
| Crystal System | Monoclinic |  |  |  |  |
| Space group | P21 |  |  |  |  |
| a / Å | 13.19743(18) | 13.1936(3) | 13.2130(3) | 13.2325(3) | 13.2688(3) |
| b / Å | 21.7622(2) | 21.7511(3) | 21.7297(3) | 21.7185(3) | 21.6763(3) |
| c / Å | 18.1487(2) | 18.1553(3) | 18.1815(3) | 18.1943(3) | 18.2309(3) |
| β / deg | 94.1520(11) | 94.2038(17) | 94.1495(18) | 94.039(2) | 93.8703(18) |
| V / Å3 | 5198.74(11) | 5196.10(16) | 5206.48(17) | 5215.87(16) | 5231.59(17) |
| Z | 2 | 2 | 2 | 2 | 2 |
| Dcalc / g∙cm-3 | 1.540 | 1.541 | 1.538 | 1.535 | 1.530 |
| μ(Mo Kα) / cm-1 | 0.837 | 0.838 | 0.836 | 0.834 | 0.832 |
| 2max / deg | 62.3520 | 61.878 | 60.702 | 61.526 | 61.938 |
| Reflections measured | 97567 | 83480 | 79833 | 82353 | 87510 |
| Independent reflections | 26744 | 26486 | 26365 | 26375 | 26468 |
| Reflections used | 26744 | 26486 | 26365 | 26375 | 26468 |
| R1 a | 0.0333 | 0.0381 | 0.0390 | 0.0379 | 0.0369 |
| Rw(F2) a | 0.0806 | 0.0900 | 0.0913 | 0.0895 | 0.0851 |
| GOF | 1.018 | 1.042 | 1.031 | 1.021 | 1.027 |
| Flack Parameter | 0.356(10) | 0.319(11) | 0.309(12) | 0.323(11) | 0.276(11) |
| CCDC No. | 2163123 | 2163124 | 2163125 | 2163126 | 2163127 |

a R1 = ||Fo| - |Fc|| / |Fo| and Rw = (|Fo| - |Fc|)2 / Fo2)1/2.

|  | 1 |  |  |  |
| --- | --- | --- | --- | --- |
| Temperature / K | 237 | 254 | 272 | 282 |
| Crystal Dimensions / mm3 | 0.6×0.6×0.6 |  |  |  |
| Chemical formula | C92H106N4Ni2O24S20 |  |  |  |
| Formula weight | 2410.42 |  |  |  |
| Crystal System | Monoclinic |  |  |  |
| Space group | P21 |  |  |  |
| a / Å | 13.3027(3) | 13.3375(3) | 13.3760(3) | 13.3988(3) |
| b / Å | 21.6453(4) | 21.6167(4) | 21.5994(4) | 21.5792(4) |
| c / Å | 18.2686(4) | 18.3081(4) | 18.3362(4) | 18.3596(4) |
| β / deg | 93.655(2) | 93.505(2) | 93.373(2) | 93.338(2) |
| V / Å3 | 5249.58(19) | 5268.58(19) | 5288.40(19) | 5299.40(19) |
| Z | 2 | 2 | 2 | 2 |
| Dcalc / g∙cm-3 | 1.525 | 1.519 | 1.514 | 1.511 |
| μ(Mo Kα) / cm-1 | 0.829 | 0.826 | 0.823 | 0.821 |
| 2max / deg | 61.4080 | 61.8740 | 61.9860 | 62.5520 |
| Reflections measured | 82444 | 85675 | 84884 | 70798 |
| Independent reflections | 26609 | 26960 | 26919 | 21627 |
| Reflections used | 26609 | 26960 | 26919 | 21627 |
| R1 a | 0.0382 | 0.0383 | 0.0391 | 0.0350 |
| Rw(F2) a | 0.0903 | 0.0879 | 0.1171 | 0.0839 |
| GOF | 0.934 | 1.018 | 0.902 | 1.018 |
| Flack Parameter | 0.321(12) | 0.337(11) | 0.299(12) | 0.248(13) |
|  | 2163128 | 2163129 | 2163130 | 2163131 |

a R1 = ||Fo| - |Fc|| / |Fo| and Rw = (|Fo| - |Fc|)2 / Fo2)1/2.

Figure S1. Temperature-dependence of β in unit cell.

Figure S2. Temperature dependence of cell parameters normalized at 118 K.

§2. Crystallographically independent molecules with atom numbering

Figure S3. Crystallographically independent molecular structure in the crystal 1 at 118 K with atomic number. (a) Molecular structure of DB3. Disordered carbon atoms depicted as yellow and blue colors. (b) molecular structures of PD2 and DB2. (c) Molecular structures of DB1, PD1A, and PD1B. (d) Atom numbering for [Ni(dmit)2] in the packing with crystallographically independent supramolecular cations.

The length of covalent bonds between the nitrogen atoms in the typical pdazH+ cations are longer than those between the nitrogen and carbon atoms. We could not assign nitrogen atoms next to N1A and N1B from the lengths of C-C and C-N bond within PD1A and PD1B due to the disorder of pdazH+. However, if we place the nitrogen atoms other than N2A and N2B, as described in Figure 2b, we could not solve the structure without using restrained commands for bond distance on Shelx refinement. On the other hand, the distance between N3 and N4 atoms in PD2 was 1.307(5) Å whereas those between N3 or N4 and adjacent carbon atoms were 1.302(6) and 1.276(6) Å, respectively. Therefore, we could safely assign the position of N4 atom of the PD2 in crystal 1. The assignment of N4 atom in PD2 is reasonable because N4 atom in PD2 contacts C-H bond in PD1A and PD1B and forms a C-H•••N interaction (Figure 2c, see also Table S3 for the details of C-H•••N4 interactions).

Table S2. Temperature-dependent C•••O distance and C-H•••O angles between PD1A•••DB3A, and PD1B•••DB3B.

|  | PD1A•••DB3A |  | PD1B•••DB3B |  |
| --- | --- | --- | --- | --- |
| T / K | C15A•••O16A distance / Å | C15A-H@•••O16A angle / ° | C13B•••O16B distance / Å | C13B•••O16B angle / ° |
| 118 | 3.154 | 134.16 | 3.322 | 153.76 |
| 135 | 3.126 | 136.24 | 3.418 | 152.91 |
| 151 | 3.132 | 134.01 | 3.409 | 154.05 |
| 169 | 3.101 | 135.80 | 3.392 | 155.84 |
| 186 | 3.089 | 133.53 | 3.410 | 152.97 |
| 194 | 3.037 | 135.47 | 3.445 | 153.81 |
| 202 | 3.031 | 134.52 | 3.451 | 154.01 |
| 221 | 3.031 | 132.98 | 3.438 | 151.70 |
| 237 | 3.035 | 132.29 | 3.364 | 141.17 |
| 254 | 3.025 | 131.19 | 3.400 | 142.78 |
| 272 | 3.084 | 130.60 | 3.380 | 139.94 |
| 282 | 3.047 | 128.51 | 3.337 | 139.23 |

Table S3. Temperature-dependent C•••N distances, and C-H•••N angles between PD1A•••PD2, and PD1B•••PD2.

|  | PD1A•••PD2 |  | PD1B•••PD2 |  |
| --- | --- | --- | --- | --- |
| T / K | C13A•••N4 distance / Å | C13A-H@•••N4 angle / ° | C16B•••N4 distance / Å | C16B-H•••N4 angle / ° |
| 118 | 3.426 | 165.05 | 3.430 | 120.16 |
| 135 | 3.415 | 166.59 | 3.462 | 120.05 |
| 151 | 3.439 | 166.13 | 3.463 | 120.30 |
| 169 | 3.536 | 163.54 | 3.431 | 120.90 |
| 186 | 3.532 | 166.32 | 3.472 | 120.34 |
| 194 | 3.531 | 166.09 | 3.487 | 120.81 |
| 202 | 3.578 | 165.91 | 3.467 | 122.87 |
| 221 | 3.588 | 165.89 | 3.541 | 120.80 |
| 237 | 3.621 | 165.86 | 3.557 | 119.83 |
| 254 | 3.600 | 164.95 | 3.790 | 118.94 |
| 272 | 3.640 | 162.61 | 3.843 | 116.02 |
| 282 | 3.684 | 164.80 | 3.719 | 118.41 |

Table S3. Temperature dependence of the parameters for N-H•••O hydrogen bonds (N•••O distance and N-H•••O angle) between PD1A•••DB1, PD1B•••DB1, and PD2•••DB2.

|  | N-H•••O hydrogen bond |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | PD1A•••DB1 |  | PD1B•••DB1 |  | PD2•••DB2 |  |
| T / K | N1A•••O20 distance / Å | N1A-H1A•••O16 angle / ° | N1B-O24 distance / Å | N1B-H1B•••O24 angle / ° | N3•••O4 distance / Å | N3-H3•••O4 angle / ° |
| 118 | 2.806 | 172.03 | 2.932 | 170.89 | 2.814 | 170.45 |
| 135 | 2.804 | 171.12 | 2.914 | 171.28 | 2.814 | 169.79 |
| 151 | 2.831 | 171.57 | 2.911 | 171 | 2.816 | 169.85 |
| 169 | 2.793 | 168.83 | 2.912 | 172.16 | 2.818 | 168.57 |
| 186 | 2.798 | 169.97 | 2.912 | 170.83 | 2.827 | 167.07 |
| 194 | 2.806 | 169.38 | 2.92 | 168.51 | 2.83 | 166.68 |
| 202 | 2.81 | 167.66 | 2.916 | 174.45 | 2.832 | 165.48 |
| 221 | 2.81 | 168.14 | 2.922 | 172.7 | 2.847 | 164.54 |
| 237 | 2.806 | 168.41 | 2.919 | 166.59 | 2.853 | 163.28 |
| 254 | 2.817 | 169.19 | 2.983 | 171.32 | 2.865 | 161.69 |
| 272 | 2.813 | 169.66 | 2.955 | 166.01 | 2.884 | 161.11 |
| 282 | 2.824 | 168.64 | 2.907 | 166.33 | 2.88 | 160.99 |

Table S5. Temperature dependence of O•••π distances between DB1•••PD1A and DB2•••PD2.

|  | DB1•••PD1A |  |  |  |
| --- | --- | --- | --- | --- |
|  | Interatomic Distance / Å |  |  |  |
| T / K | O18•••C13A | O18•••C14A | O22•••C13A | O22•••C14A |
| 118 | 2.999 | 3.022 | 2.908 | 3.057 |
| 135 | 2.969 | 3.038 | 2.941 | 3.036 |
| 151 | 2.984 | 3.038 | 2.936 | 3.048 |
| 169 | 2.979 | 3.039 | 2.929 | 3.058 |
| 186 | 3.021 | 3.054 | 2.902 | 3.054 |
| 194 | 3.027 | 3.016 | 2.901 | 3.112 |
| 202 | 3.026 | 3.045 | 2.901 | 3.083 |
| 221 | 3.048 | 3.053 | 2.894 | 3.081 |
| 237 | 3.031 | 3.019 | 2.92 | 3.124 |
| 254 | 3.052 | 3.022 | 2.93 | 3.132 |
| 272 | 3.091 | 3.019 | 2.91 | 3.143 |
| 282 | 3.055 | 3.028 | 2.937 | 3.125 |

|  | DB2•••PD2. |  |  |  |
| --- | --- | --- | --- | --- |
|  | Interatomic Distance / Å |  |  |  |
| T / K | O6•••C17 | O6•••N3 | O2•••C20 | O7•••C20 |
| 118 | 3.192 | 3.092 | 3.057 | 3.192 |
| 135 | 3.202 | 3.096 | 3.055 | 3.194 |
| 151 | 3.19 | 3.092 | 3.054 | 3.197 |
| 169 | 3.202 | 3.083 | 3.049 | 3.195 |
| 186 | 3.212 | 3.075 | 3.047 | 3.19 |
| 194 | 3.22 | 3.073 | 3.041 | 3.188 |
| 202 | 3.224 | 3.068 | 3.045 | 3.187 |
| 221 | 3.237 | 3.059 | 3.046 | 3.174 |
| 237 | 3.241 | 3.054 | 3.045 | 3.177 |
| 254 | 3.247 | 3.042 | 3.05 | 3.17 |
| 272 | 3.25 | 3.038 | 3.048 | 3.176 |
| 282 | 3.259 | 3.038 | 3.053 | 3.17 |

§3. Input and output file of PASCal Calculation, and indicatrix plots

Table S6. Input and output file of PASCal Calculation for structural data of 1 between 118 and 169 K.

| input | T / K | σT | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 169 | 5 | 13.162 | 21.7862 | 18.1119 | 90 | 94.3187 | 90 |
|  | 151 | 5 | 13.139 | 21.805 | 18.0856 | 90 | 94.4155 | 90 |
|  | 135 | 5 | 13.1146 | 21.8149 | 18.0621 | 90 | 94.502 | 90 |
|  | 118 | 5 | 13.0944 | 21.8192 | 18.0486 | 90 | 94.607 | 90 |

| output |  |  |  |  | Direction |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Axes | α / MK–1 | σα / MK–1 | a | b | c |
|  | X1 | -29.6503 | 4.1985 | 0 | 1 | 0 |
|  | X2 | 38.0421 | 3.9509 | -0.6675 | 0 | 0.7446 |
|  | X2 | 142.2858 | 1.4664 | 0.8931 | 0 | 0.4499 |
|  | V | 151.2583 | 2.7976 |  |  |  |
|  | % change in length |  |  |  |  |  |  |
|  | T / K | X1 | X2 | X2 | X1,calc | X2,calc | X3,calc |
|  | 118 | 0 | 0 | 0 | 0.0159 | -0.0179 | -0.0069 |
|  | 135 | -0.0197 | 0.0215 | 0.2221 | -0.0345 | 0.0468 | 0.235 |
|  | 151 | -0.0651 | 0.1047 | 0.4674 | -0.082 | 0.1077 | 0.4626 |
|  | 169 | -0.1512 | 0.1865 | 0.72 | -0.1354 | 0.1761 | 0.7188 |
|  | Volume |  |  |
|  | T / K | V / Å3 | Vlin / Å3 |
|  | 118 | 5139.993 | 5139.4723 |
|  | 135 | 5151.509 | 5152.6892 |
|  | 151 | 5166.071 | 5165.1287 |
|  | 169 | 5178.84 | 5179.1231 |

Table S7. Input and output file of PASCal Calculation for structural data of 1 between 186 and 282 K.

| input | T / K | σT | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 282 | 5 | 13.3988 | 21.5792 | 18.3596 | 90 | 93.338 | 90 |
|  | 272 | 5 | 13.376 | 21.5994 | 18.3362 | 90 | 93.373 | 90 |
|  | 254 | 5 | 13.3375 | 21.6167 | 18.3081 | 90 | 93.505 | 90 |
|  | 237 | 5 | 13.3027 | 21.6453 | 18.2686 | 90 | 93.655 | 90 |
|  | 221 | 5 | 13.2688 | 21.6763 | 18.2309 | 90 | 93.8703 | 90 |
|  | 202 | 5 | 13.2325 | 21.7185 | 18.1943 | 90 | 94.039 | 90 |
|  | 194 | 5 | 13.213 | 21.7297 | 18.1815 | 90 | 94.1495 | 90 |
|  | 186 | 5 | 13.1936 | 21.7511 | 18.1553 | 90 | 94.2038 | 90 |

| output |  |  |  |  | Direction |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Axes | α / MK–1 | σα / MK–1 | a | b | c |
|  | X1 | -81.2513 | 2.7 | 0 | 1 | 0 |
|  | X2 | 55.4528 | 3.149 | -0.738 | 0 | 0.6749 |
|  | X2 | 230.0634 | 3.3742 | 0.859 | 0 | 0.512 |
|  | V | 204.178 | 1.9955 |  |  |  |
|  | % change in length |  |  |  |  |  |  |
|  | T / K | X1 | X2 | X2 | X1,calc | X2,calc | X3,calc |
|  | 186 | 0 | 0 | 0 | -0.0324 | 0.018 | 0.028 |
|  | 194 | -0.0984 | 0.1015 | 0.1967 | -0.0974 | 0.0624 | 0.2121 |
|  | 202 | -0.1499 | 0.1152 | 0.4153 | -0.1624 | 0.1068 | 0.3961 |
|  | 221 | -0.3439 | 0.2107 | 0.817 | -0.3168 | 0.2121 | 0.8333 |
|  | 237 | -0.4864 | 0.2644 | 1.2529 | -0.4468 | 0.3008 | 1.2014 |
|  | 254 | -0.6179 | 0.3778 | 1.6376 | -0.5849 | 0.3951 | 1.5925 |
|  | 272 | -0.6974 | 0.4775 | 1.9988 | -0.7312 | 0.4949 | 2.0066 |
|  | 282 | -0.7903 | 0.5935 | 2.1883 | -0.8124 | 0.5504 | 2.2367 |
|  | Volume |  |  |
|  | T / K | V / Å3 | Vlin / Å3 |
|  | 186 | 5196.1057 | 5196.7608 |
|  | 194 | 5206.4888 | 5205.2482 |
|  | 202 | 5215.8741 | 5213.7356 |
|  | 221 | 5231.5855 | 5233.8933 |
|  | 237 | 5249.5783 | 5250.8682 |
|  | 254 | 5268.5849 | 5268.904 |
|  | 272 | 5288.3999 | 5288.0008 |
|  | 282 | 5299.4039 | 5298.6101 |

Figure S4. Indicatrix plots for structural data of 1 between (a) 118 and 169 K and (b) 186 and 282 K.

PASCal Indicatrix Plotter was used to plot the data. The software was obtained from the web site: https://cliffe.nottingham.ac.uk/programs/

§4 Differential scanning calorimetry (DSC) for crystal 1

Figure S5. Differential scanning calorimetry from 150 to 290 K. Red and blue allows indicate the heating and cooling processes, respectively.

§5 Temperature-dependence of structural change between PD1B•••DB3B and PD1B•••PD2.

Figure S6. Schematic of selected parameters in supramolecular cation structure. The atoms are displayed using the thermal ellipsoid model. (a) Schematic of the interaction (purple) between C16B in PD1B and N4 in PD2 (dC-N). (b) Temperature dependences of ΨPD1B (Green), and dC-N (purple). The dashed line corresponds to the phase transition temperature of 183 K.

§6 Transfer integrals (t) between [Ni(dmit)2]– anions and their temperature dependence.

Figure S7. Transfer integrals (t) between [Ni(dmit)2]– anions and their temperature dependence. (a) Arrangement of [Ni(dmit)2]– and corresponding t (tintra, t2, t3, and t4), where tintra represents t in intradimer. (b) Temperature-dependent t. Each t corresponds to those in (a).

§6 Expanded χmT versus T plot of Figure 5.

Figure S8. Expanded χmT versus T plot of Figure 5 with the left axis expanded from 0.65 to 1.0 cm3 K mol–1. Black and blue lines represent the singlet-triplet (S-T) thermal excitation models explained in the main text.

Singlet-triplet (S-T) thermal excitation model is described as follows S1:

m=2NAμB2g2kBT1[3+exp⁡(-2J/kBT)]

where NA, μB, g, and kB are Avogadro number, Bohr magneton, Landé g-factor, and Boltzmann constant, respectively. In the modified model, J/kB = c0 T + c1 are used, where c0 and c1 are constant.

References

[S1] B. Bleaney, K. D. Bowers, Proc. R. Soc. Lond. A, 1952, 214, 451–465.